| Energy | Be | Ni Error: Reference source not found | Air Error: Reference source not found |  |  | Air |
| --- | --- | --- | --- | --- | --- | --- |
| MeV | MeV/ g/cm2 | MeV/ g/cm2 | MeV/ g/cm2 |  |  | Range g/cm2 |
| 1 | 1.48 | 1.35 | 1.67 |  |  | .55 |
| 5 | 1.56 | 1.64 | 1.91 |  |  | 3.1 |
| 10 | 1.67 | 2.00 | 2.16 |  |  | 6.3 |
| 20 | 1.84 | 2.70 | 2.54 |  |  | 12.0 |
| Conversion: MeV/g/cm2  keV/m | 0.185 | 0.889 | .00012 |  | Conversion g/cm2  m | 8.25 |
| MeV | keV/m | keV/m | MeV/m |  |  | m |
| 1 | 0.27 | 1.20 | 0.20 |  |  | 4.5 |
| 5 | 0.29 | 1.45 | 0.23 |  |  | 25 |
| 10 | 0.31 | 1.78 | 0.26 |  |  | 52 |
| 20 | 0.34 | 2.4 | 0.30 |  |  | 100 |
| Conversion: keV/m  Watts/mA-m | 1.00 | 1.00 | 1000 |  |  |  |
| MeV | Watts/mA-m | Watts/mA-m | Watts/mA-m |  |  |  |
| 1 | 0.27 | 1.20 | 200 |  |  |  |
| 5 | 0.29 | 1.45 | 230 |  |  |  |
| 10 | 0.31 | 1.78 | 260 |  |  |  |
| 20 | 0.34 | 2.4 | 300 |  |  |  |
| Density (g/cm3) | 1.85 | 8.89 | .001205 |  |  |  |

1 mA = 6.2E15 electrons/sec

1 keV = 1.6E-16 joules

1 joule/sec = 1 watt

Total energy loss = (Current [e/sec]) (dE/dx [keV/m]) (j/keV-sec) (Watts/(j/sec)) = Watts/m

Assuming: 1mA electron current with dE/ex = 1 keV/m, then:

Energy loss = (6.2E15 e-/sec) (1 keV/m) (1.6E-16 j/keV) = 1 Watt/m

Beam Heating of Foil

Energy Deposited by Beam in the Foil

- For 20 MeV, 1mA electrons in Be foils, 0.34 watts are deposited/m of foil.

- This energy will be distributed over the beam volume, V = ATx10-4 cm3, where A is the beam area (cm2) and T is the foil thickness (um)

Foil Heating

- Be specific heat = 1.83 J/(ΔC g)    [1.83J will raise 1gram of Be by 1 oC]

- Be density = 1.85 g/cm3.

- Be mass transited by the Beam = ρV = (1.85 g/cm3)(ATx10-4 cm3)] = 1.85x10-4 AT g

- Temperature rise (ΔC)	= [Heat/gram] / Specific Heat

= [(0.34 T J / sec) /(1.85x10-4 AT g)] / [1.83 J / ΔC g]

=  2954 (Current (mA))(dE/dx (Watts/mA-m)) / A(cm2) )  ΔC / sec

EXAMPLES

For a Be foil, with a 20 MeV, 10 uA beam about 3 mm in diameter (A = .07 cm2) :

- Temperature rise (ΔC)	= 2954 (.01)(.34) / (.07) ΔC / sec

= 140  ΔC / sec

For a Be foil, with a 5 MeV, 10 uA beam about 0.3 cm in diameter (A = .07 cm2) :

- Temperature rise (ΔC)	= 2954 (.01)(.27) / (.07) ΔC / sec

= 110  ΔC / sec

- Assume a ROTATING FOIL at radius 1”, with an electron beam diameter of 3mm.

  - The beam track = 160 mm. This is 53 beam diameters (3 mm beam).

- Beryllium Melting Point = 1287 °C

- Temperature rise to ¼ melting = 316 °C

Beryllium Window Temperature Increase

(Note : Temp. Rise is Independent of Be Thickness)

|  |  | Non-Rotating Window |  | Rotating Window |  |
| --- | --- | --- | --- | --- | --- |
| Beam Energy | Beam Current | Temp Rise / sec | Time to ¼ Melting | Temp Rise / sec | Time to ¼ Melting |
| 6 MeV | 1 A | 11 oC / sec | 28 sec | 0.20 oC / sec | 25 min |
|  | 10 A | 110 oC / sec | 3 sec | 2.0 oC / sec | 150 sec |
|  | 100 A | 1,100 oC / sec | 0 | 20.7 oC / sec | 15 sec |
|  | 1 mA | 11,000 oC / sec | 0 | 207 oC / sec | 1 sec |
| 18 MeV | 1 A | 14 oC / sec | 23 sec | 0.26 / sec | 20 min |
|  | 10 A | 140 oC / sec | 2 sec | 2.6 oC / sec | 120 sec |
|  | 100 A | 1,400 oC / sec | 0 | 26 oC / sec | 12 sec |
|  | 1 mA | 14,000 oC / sec | 0 | 260 oC / sec | 1 sec |

“Stopping Powers for Electrons and Positrons”, M. Berger, ICRU-37 , Washington D.C., 1984

Same as (1). The author notes that the Ranges are not backed by experimental data, and may be inaccurate.